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Serbuk gergaji merupakan limbah industri penggergajian kayu. Limbah serbuk gergaji cukup banyak menimbulkan masalah dalam penanganannya yang selama ini dibiarkan membusuk, ditumpuk dan dibakar. Penanganan tersebut dapat membuat kondisi lingkungan sekitar menjadi tidak baik. Penelitian ini memanfaatkan limbah serbuk gergaji sebagai bahan tambah dalam campuran beton. Serbuk gergaji yang ditambahkan dalam campuran beton diharapkan dapat meningkatkan kekuatan beton.
Penelitian ini menggunakan serbuk gergaji kayu jati sisa pengergajian pengrajin furniture. Penambahan serbuk gergaji yang digunakan sebanyak 0%; 0,25%; 0,5%; 0,75%; dan 1% dari berat total agregat beton. Variasi penambahan serbuk gergaji dilakukan untuk mengetahui pengaruhnya terhadap kuat tekan, kuat tarik belah, modulus elastisitas, penyerapan dan porositas beton. Penelitian ini juga menggunakan superplasticizer untuk meningkatkan kelacakan campuran beton dikarenakan adanya penambahan serbuk gergajiyang memiliki penyerapan cukup tinggi. 
Hasil pengujian menunjukkan peningkatan kuat tekan pada variasi serbuk gergaji 0,25% sebesar 29,28% dan pada penambahan serbuk gergaji berikutnya cenderung mengalami penurunan, namun nilai kuat tarik beton cenderung mengalami penurunan dari kuat tarik beton tanpa serbuk gergaji. Pada pengujian penyerapan dan porositas beton menunjukka nilai penyerapan dan porositas beton semakin meningkat seiring penambahan serbuk gergaji.
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	Sawdust is a sawmill waste industry. Sawmill waste causes a lot of problems in handling it which has been left to decompose, stacked and burned.That handling can make surrounding environment not good. This research uses sawdust as additive in concrete mix. Using this sawdust as additive is expected to increase the strength of concrete.
	This research used sawdust of teak wood leftovers from furniture craftsmen. The addition of sawdust used is 0%; 0.25%; 0.5%; 0.75%; and 1% of total weight the aggregate. Variations in the addition of sawdust were carried out to determine its effect on compressive strength, split tensile strength, modulus of elasticity, absorption and porosity of concrete. This research also used superplasticizer to improve the workabilitys of concrete mixtures due to the addition of sawdust which has high absorption.
	From the result of this research showed an increase in compressive strength in the 0.25% variation of sawdust by 29.28% and the addition of subsequent sawdust tends to decrease the compressive sterngth, but the tensile strength values ​​of the concrete tend to decrease from the tensile strength of concrete without sawdust. In the absorption and porosity testing of concrete showed the value of absorption and porosity of concrete increases with the addition of sawdust.
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